## Slide 1: Iron and Steel
Magnet and Steel, Walter Egan

## Slide 2: Properties of Iron and Steel
Hard
Opaque
Malleable
Metallic
Electrical Conductor
Thermal Conductor
Magnetic
Strong

## Slide 3: Iron and Steel
The transition from the Bronze Age to the Iron Age was ushered in by two developments:
  Growing scarcity of copper and/or tin
  Increased processing temperatures
Iron and Steel Characteristics?
What is the difference?

## Slide 4: Iron vs Steel
Bronze was an Alloy of Cu
  Arsenic or Tin most common alloying impurity
Steel is an Alloy of Iron
  Carbon is the most common alloying impurity
Iron and Carbon is probably the most useful combination in the history of Society
Terms you should know
  Forging – beating or hammering a material into shape
  Casting – Pouring a liquid into a mold

## Slide 5: Forms of iron
Who has heard these terms?
  Wrought Iron
  Steel
  Cast Iron
  What is the Difference?
  The Amount of Carbon

## Slide 6: Forms
Low Carbon 0-0.2%
  Wrought Iron
  Pure, Ductile, typically about as strong as Bronze
  High melting point (>1500°C)
Medium Carbon 0.2-2.1%
  Steel
  Very strong, hard, forgable,
  1000X harder than pure Fe
  High melting point (>1400°C)
High Carbon 2.3-4.3%
  Cast Iron or Pig Iron
  Low Melting Point, Brittle, Not Forgable
  Can only be Cast

## Slide 7
The Iron-Iron Carbide Phase Diagram
Wrought
Iron
Steel
Cast Iron
http://d2vlcm61l7u1fs.cloudfront.net/media%2F5fa%2F5fabc8f5-c63b-4e9b-b65c-d05ad2626ae5%2FphpSvCYaJ.png
Notes: f24_09_pg290.jpg

## Slide 8
Why is Steel Strong?
Two Important phases of iron-  - Ferrite (BCC) - Austenite (FCC)
How much carbon can you dissolve in the Iron?
Ferrite very little (<0.02%)
Austenite Lots (up to 2.1%)
Why is that important?
When you heat Steel to 1000°C what phase do you have?
Austenite with lots of Carbon
When you cool it what does the carbon do?
It can precipitate into Carbide particles. Strains crystal makes dislocation motion difficult (hardens)
Wrought Iron
Steel
Cast Iron
Austenite
Ferrite
http://d2vlcm61l7u1fs.cloudfront.net/media%2F5fa%2F5fabc8f5-c63b-4e9b-b65c-d05ad2626ae5%2FphpSvCYaJ.png
Notes: f24_09_pg290.jpg

## Slide 9: Forms of iron
Wrought Iron (Paper Clip)
  Very little carbon (<0.2%)
  Difficult to slow the dislocations since carbon is dissolved
  Soft, malleable, easily wrought
Steel (Bobby Pin)
  Medium carbon (0.2-2.3%)
  Can dissolve carbon in Austenite but it wants to precipitate upon cooling
  Properties depend on how fast you cool
  Strain from Carbides greatly strengthens the steel
  Must control both the amount of carbon and the tempering
Cast Iron
  High Carbon (2.3-4.3%)
  Forms lots of carbide phase
  Make the material brittle (too much of a good thing)

## Slide 10: Why is the Heat treatment important?
For Steel if you heat it to 1000°C you make Austenite
  Slow Cool (annealing)
    For both Bobby pin (high C) and Paper Clip (low C)
      Annealing removes dislocations
      Give it time for the Carbon to form particles
      Makes material softer
      Slightly stronger than Bronze
  Fast Cool or Quench
    For Bobby Pin
      Transform to Martensite
      Excess Carbon strains martensite (brittle)
    For Paper Clip
      Transform to Martensite but less excess carbon (less brittle)
  Tempering
    Heat again to move carbon around and restore ductility

## Slide 11
Why is Steel Strong?
Two Important phases of iron-  - Ferrite (BCC) - Austenite (FCC)
How much carbon can you dissolve in the Iron?
Ferrite very little (<0.02%)
Austenite Lots (up to 2.1%)
Carbon makes Paper clips harder and bobby pins brittle when quenched
Stuck in interstitial positions
Iron
Steel
Cast Iron
Austenite
Paper
clip
Bobby
pin
http://d2vlcm61l7u1fs.cloudfront.net/media%2F5fa%2F5fabc8f5-c63b-4e9b-b65c-d05ad2626ae5%2FphpSvCYaJ.png
Notes: f24_09_pg290.jpg

## Slide 12: So how do you make Iron?
Start with
  Iron Oxide (either Fe2O3 or Fe3O4), (mineral form is Taconite)
  Limestone (CaCO3, Oyster Shells) and
  Carbon (Charcoal)
Layer these and light on fire and use bellows to get hot
2C +O2=> 2CO (our favorite reducer)
Fe2O3 +3CO => 2 Fe +3CO2 (reduction makes Iron)
Now have to get rid of sand (impurity that comes with iron ore)
CaCO3 => CaO +CO2 (make lime)
CaO + SiO2 => CaSiO3 (glass slag)

## Slide 13: Methods of Making and Manipulating Iron
Bloomery Furnace
  Makes wrought iron (Low Carbon)
Blast Furnace
  Makes Cast Iron (High Carbon)
Finery Forge
  Converts Cast iron to Wrought Iron
Carburization
  Converts wrought iron to steel
Bessimer Furnace
  Converts Cast Iron to Steel (medium carbon)

## Slide 14: Wrought Iron: Early Bloomeries
Bloom Iron/Wrought Iron
  Make a Bloom by heating the mixture we just described
  Beat on the bloom with a hammer to separate the iron from the silicate slag
  Left with pure wrought (low carbon) iron
  Bloom Iron Video

## Slide 15: Blast Furnace
Blast Furnace
  Same ingredients (Iron Ore, Charcoal and Limestone)
  Heat hotter and collect liquid iron from bottom
  Cast Iron is also called Pig Iron
  Chinese skipped Bloomery stage and just made cast iron from ancient blast furnaces
  Not seen in Europe until 1500’s
Finery Forge
  Now you have too much carbon
  Use Finery Forge to remelt pig iron,
  oxidize carbon and silicon
  Make bloom and beat it, create wrought iron

## Slide 16: Bloom vs Blast
In Bloomary you can’t get to the melting point of wrought iron: must beat it out
In Blast Furnace you can get to the melting point of cast iron: make pig iron
Steel
Cast Iron
Austenite
Wrought Iron
Melting Point
Cast Iron
Melting Point

## Slide 17: Blast Furnace
Early Blast Furnace
http://media-3.web.britannica.com/eb-media/39/1539-004-7C917766.jpg
www.britanica.com
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 18: Finery Forge
Finery Forge
  With Cast Iron you have too much carbon
  Use Finery Forge to remelt pig (cast) iron,
  oxidize carbon and silicon
  Make bloom
  Beat it with water powered hammers
  Create wrought iron

## Slide 19: Converting Wrought Iron to Steel
Can make wrought iron by either beating a bloom or using a finery forge. Not enough carbon for steel
How do you make steel?
Carborization
  Need to add carbon to make steel
  Melting point too high until 1700’s
  Heat Iron in Carbon rich air – Carborization
  Carbon diffuses into the iron making outer layer of steel
  Skilled craftsmen

## Slide 20: History of Iron and Steel
3500BC Beads in Ancient Egypt for iron
  From Meteor (nickel content)
First Iron Production 3000BC Syria and Mesopotamia
Hittites mass produced Iron 1500-1200BC
  Bloom Iron in small batch process
  Use water power to beat blooms
China starts Iron age later around 700BC
  Used the first blast furnaces to make cast iron
  Also used Finery forges to make wrought iron 300BC
Wootz Steel 600BC
  Southern India, great combination of natural minerals
  Produced fine dispersion of carbides, Damascus Swords

## Slide 21: History Continued
By 1400’s needs increased
  Church bells, cannons etc
  Blast furnace developed (Cast Iron)
By 1500’s Japan is making the strongest Steel in the world
  Samuri Sword take a week just make the iron
  Use Magnetite (black sand Fe2O3) and charcoal
  Broad range of carbon, separate it by feel and sound
  Make the center from low carbon ductile steel
  Then add high carbon hard/brittle steel to outside
  Create a composite and the best steel for several hundred years

## Slide 22: History Continued
1588 Queen Elizabeth limits use of Timber
  By 1700’s have a timber famine (charcoal)
Why not use Coal?
  Too much Sulfur weakens steel along grain boundaries
  Coke the coal,
    Drives off impurities (thanks to beer)
1709 Darby England
  Low sulfur coke
  Cast iron becomes cheap
  Start of Industrial revolution
    Over 200 years
    income increases 10X
    Population increases 6X
    Machine based economy
    Free market, rule of law, no trade barriers

## Slide 23: History continued
Puddling
  Invented in 1784
  Stir Molten Pig (Cast) iron in oxidizing atmosphere
  Observe it “come to nature”
  Gather in a puddling ball
Replaced by the Bessemer Furnace 1855
  Blow Air through the melt
  Rapidly remove carbon and silicon
  Initially didn’t work tough to remove just the right amount
  Instead decided to remove it all and add carbon back
  Steel very fast (in 20 minutes) and efficient
Bessemer Furnace Video

## Slide 24: Forms
Low Carbon 0-0.2%
  Wrought Iron
  Pure, Ductile, typically about as strong as Bronze
  High melting point (>1500°C)
  Product of Bloomery
Medium Carbon 0.2-2.1%
  Steel
  Very strong, hard, forgable,
  1000X harder than pure Fe
  High melting point (>1400°C)
  Created by the Bessemer Process
High Carbon 2.3-4.3%
  Cast Iron or Pig Iron
  Low Melting Point, Brittle, Not Forgable
  Can only be Cast
  Product of Blast Furnace

## Slide 25: Methods of Making and Manipulating Iron
Bloomery Furnace
  Makes wrought iron (low carbon)
Carburization
  Converts wrought iron to steel
Blast Furnace
  Makes Cast Iron (High Carbon)
Finery Forge
  Converts Cast iron to Wrought Iron
Bessimer Furnace
  Converts Cast Iron to Steel (medium carbon)

## Slide 26: Today
Today we use 1950’s Process
  Basic Oxygen Process (BOP)
  Inject pure Oxygen
  Add alloying agents and carbon after removing carbon
US Steel Video